03/12

www.colourcraftltd.com                                                 enquiries@colourcraft-ltd.com

Pure Concentrated Denim Dye:

Ideal for Denim Jeans that have faded

and also on cotton, for tie dye etc.

Safe and easy alternative to Indigo dyeing.

TRADITIONAL METHOD – (known as exhaust dyeing)

- Weigh fabric dry weight, then thoroughly wash, rinse and leave damp.

- Measure 2 litres of warm water (30°C) for every 100g dry weight of fabric into the dye

bath.

- From the Shade Guide table below, weigh out the required amount of dye for the shade required.

- In a separate container, dissolve the required amount of dye in warm water until fully solubilised.

- Immerse fabric in dye bath and agitate well.

- Slowly raise the temperature of the dye bath to 60(C over 45 minutes. OR if this is not possible use hot water at step 2 and leave in this water to soak for at least 1 hour.

- Move the material through the liquid every few minutes to ensure even dyeing and until the shade required is achieved.

- Finish with a cool rinse and then a thorough hot wash (adding 2g per litre of Colsperse scouring and rinsing agent or detergent to the water), rinse, dry and iron.

APPROXIMATE SHADE GUIDE

|  | Dye gms. | Fabric dry weight gms |
| --- | --- | --- |
| Pastel shade | 25g | 100g |
| Medium shade | 30g | 100g |
| Deep shades | 40g | 100g |

It is always advisable to weigh each individual item to be dyed, however the table below gives a rough guide on the weight of a range of items.

APPROXIMATE WEIGHT GUIDE

| Item | Weight gms | Amount of dye for Deep Shade gms |
| --- | --- | --- |
| Jeans or Trousers | 600g | 250g |
| 2 Shirts | 500g | 200g |
| Bath Towel | 600g | 250g |
| Double Sheet | 600g | 250g |
| Double Duvet Cover | 1200g | 480g |
| Curtains | 2kg | 800g |

SAFETY IN USE

COLOURCRAFT DENIM DYE IS NON-TOXIC WHEN USED PROPERLY.

Care should be taken when handling all dyes/associated chemicals – THE USE OF RUBBER GLOVES AND PROTECTIVE CLOTHING IS RECOMMENDED. Precautions MUST be taken to avoid accidental ingestion, inhalation and skin and eye contact.  Keep containers closed and away from children.  Information contained in this publication or as otherwise supplied is believed to be accurate and is given in good faith, but without guarantee as we have no control over conditions of use and individual application.