UNIT 5,  555 CARLISLE STREET EAST, SHEFFIELD  S4 8DT.

TEL:  0ll4 242 l43l   FAX:  0114 243 4844

Email:  enquiries@colourcraft-ltd.com

Website:  www.colourcraftltd.com

Dip Dyeing with Disperse/ Transfer Dyes

In addition to using as transfer dyes, disperse dyes can be used for dyeing polyester or polyester/cotton mix.

We strongly recommend performing a trial run on a scrap piece of fabric.

Method:

1.Prewash fabric and leave damp.

2. Put sufficient  boiling water into a stainless container to allow free movement of the cloth, however, water can be added after steps 3 and 4 to ensure this.

3. Add disperse dye and mix until thoroughly dissolved. (see below)

4.Add the fabric to the dyebath and gently stir.

5. For best results bring to the boil over a heat source. (see below for length of time)

| SHADE | DYE (Per 100g Dry Weight of Cloth) | TIME IF BOILING FABRIC (Best Result) |
| --- | --- | --- |
| Pale | 2g | 10 minutes |
| Medium | 5g | 20 minutes |
| Deep | 10-15g | 40 minutes or until shade required is obtained |

Information contained in this publication or as otherwise supplied is believed to be accurate and is given in food faith, but without guarantee, as we have no control over conditions of use and individual application.